Specifications for Sound Solution Rubber

Acoustic Sound Underlay provides a superb sound barrier when installed under laminate flooring, engineered wood, or hardwood floors. Acoustic Sound absorbs and reduces the transmission of noise associated with normal foot traffic, further enhancing the acoustic ambiance of the space in which it is installed. Acoustic Sound should be installed in accordance with the flooring manufacturer’s published instructions. This product is designed for floating floor, glue in, snap in, or double glue installation.

- Materials - High Density Natural Rubber with moisture barrier

- Roll Size – 39.37” x 393.7” (100 sf per roll)

- Density – pcf – 44lbs

- Thickness (in inches) – 0.25mm/0.10 (+/- 5% manufacturing tolerance)

- Mold and mildew resistant

- Impact sound transmission

- Class (IIC) = 71

- ASTM – E492-90 (ASTM-E989-89)

- Sound Transmission Loss

- Class (STC) = 73

- ASTM-E90-02 (ASTM-E413-87)

- “R” Value – 3.19 (ft2 – f – hr/Btu-in)